In order:

Hypothesis so far: it's the epoxy and epoxy attachment that determines our strength of connection -> maybe add hardware or grooves to 3d prints?

Small wrapped:

3D:  epoxy broke at 210, no break on the carbon member or 3d print (can even reuse the carbon member) -> note that it was a break of the epoxy and the member was still very tightly connected (had to twist and turn the member to get it out of the tension connection)

Aluminum: the top lip epoxy is noticeably off (might have been pulling through the weld) after about 500 -> much hard to twist and pull out and noticeably still held together due to grooves in the aluminum connection a

Large pultruded:

3D print:

Ripped out really easily (no internal scoring meant that the epoxy did not have much to rip/grab onto) -> didn't break member or 3d print

Aluminium:

The bottom weld needed to be gone through before we got to actual data for epoxy (post 300)

Not necessarily broken, just the bond is beginning to break up (let go of pultruded large and pultruded in general)

Large wrapped:

3D print:

Top part cleanly sheared off -> not a problem with the epoxy at all (NEED TO FIX THE ANGLES OF THE DROP OFF)

Aluminum:

Popped at 560, same bottom shear issue where we have a region of getting through the weld area