## How to Join Two Rigid Carbon Fiber Sheets Using Epoxy and Flexible Carbon Fiber

This guide explains how to structurally join two rigid carbon fiber sheets using epoxy resin and flexible carbon fiber fabric as a bonding bridge.

### Materials Needed:

- Two rigid carbon fiber sheets (clean and dry)

- Flexible carbon fiber fabric (e.g., woven twill or plain weave)

- Epoxy resin system (structural, slow-curing recommended)

- Mixing cups, gloves, brush or squeegee

- Sandpaper (80–120 grit) or scuff pad

- Acetone or isopropyl alcohol (for surface cleaning)

- Peel ply (optional)

- Clamps or vacuum bagging setup (optional, for better bonding)

### Step-by-Step Instructions:

#### 1. Surface Preparation

- Sand the bonding areas on each rigid carbon fiber sheet with 80–120 grit sandpaper to promote adhesion.

- Clean the sanded surfaces thoroughly with acetone or isopropyl alcohol to remove dust, oils, and debris.

- Dry-fit the sheets to check alignment and spacing. Make sure the flexible fabric can span the gap with at least 1 inch (25 mm) of overlap on each side.

#### 2. Cut the Flexible Carbon Fiber

- Cut one or more strips of flexible carbon fiber fabric wide enough to bridge the joint.

- Ensure at least 1 inch of overlap on both sides of the joint for adequate bonding area.

- Use multiple layers if increased joint strength is required.

#### 3. Mix the Epoxy Resin

- Mix the epoxy according to the manufacturer’s instructions, using the correct ratio of resin to hardener.

- Allow the mixture to rest briefly to reduce bubbles.

#### 4. Wet Out the Materials

- Use a brush or squeegee to thoroughly wet out the flexible carbon fiber fabric with epoxy.

- Apply a coat of epoxy to the sanded bonding areas of both rigid carbon fiber sheets.

#### 5. Apply the Flexible Carbon Fiber

- Carefully position the wetted fabric strip across the joint so that it adheres to both rigid sheets.

- Press the fabric down to eliminate air bubbles and ensure full contact with the bonding surfaces.

- Apply more resin as needed to eliminate dry spots, but avoid excessive saturation.

#### 6. Consolidation (Optional but Recommended)

- For improved compaction and finish, place peel ply over the joint and apply pressure using clamps or a vacuum bag.

- If vacuum bagging is not used, apply even pressure using weights or clamps to ensure good contact during cure.

#### 7. Curing

- Allow the epoxy to cure fully according to the resin manufacturer’s schedule (typically 12–24 hours at room temperature).

- Avoid moving or disturbing the joint during the curing process.

#### 8. Finishing (Optional)

- Once cured, excess epoxy or rough edges can be trimmed or sanded.

- For a clean appearance and environmental resistance, consider applying a UV-protective clear coat.

### Tips for Strength and Durability:

- Ensure generous overlap—more surface area equals a stronger joint.

- Multiple fabric layers can significantly increase bond strength.

- Use structural-grade epoxy (e.g., West System 105/206 or Pro-Set).

- Avoid fast-setting epoxies; they tend to have lower bond strength.

- Test the joint if it's going to be under significant load.